TRS TYPE C45, 2 SHEAR CONNECTORS, 1 SLOT, CATEGORY 3

(e)

RODS

(c)	(d)

(g)

(b)

(f)	(a)

EXISTING TIMBER TO BE SLOTTED IN SITU	TRS - RODS FACTORY BONDED

COMPANY - Bramble Construction CONTACT - Martin Waller

SITE - Unspecified DATE - 28/07/26

| BEAM REFERENCE NO. 1 45 degree special | NO. TO REPAIR 10 |
| --- | --- |
| DIMENSIONS (NOT TO SCALE) |  |
| WIDTH (mm) (a) | 75 |
| DEPTH (mm) (b) | 200 |
| OVERALL LENGTH (mm) | 500 |
| BASE THICKNESS (mm) (c) | 40 |
| SHEAR CONNECTOR (ROD) CENTRES (mm) (d/e) | 50/150 |
| SHEAR CONNECTORS (RODS) |  |
| LENGTH OVERALL (mm) (50:50 EXISTING/TRS) | 300(TOP) 400(BOT) |
| DIAMETER (mm) | 16 |
| NUMBER | 2 |
| MATERIAL | EPOXY/STEEL |
| SLOTS (DO NOT SCALE FROM SKETCH) |  |
| NUMBER | 1 |
| WIDTH (mm) (f) | 25 |
| DEPTH (mm) (g) | 165 |

SCHEMATIC ONLY - NOT TO SCALE	ãD C MOORE 1997

ALL PROPOSALS TO BE VERIFIED BY A STRUCTURAL ENGINEER