- Course help - David Moore - 01626 331351 - dcmoore@timber.org.uk

AN ANSWER TO ROT
Exercise 3

  You are standing on the first or ground floor of a building with the following tools: a torch, a tape measure, a 'damp' testing meter, a screwdriver, plus a pad and pencil.

(Use the attached form to make notes as you go and then compare them with the suggested answers).

- What you can see

Floor boards laid over timber joists. The joists may be supported in the middle by a larger 'carrier' beam.

- Checking for defects

You notice that the joists look creased and light coloured  where they disappear into the wall (wall socket or bearing).

Q.  What other symptoms of decay or attack might you notice?

A. Mould (white), splitting or cracking (into cubes), insect holes of various sizes, sagging of the floor and cracks in the ceiling, smell, strands, mushrooms or ‘skins’ (mycelium) of Dry or Wet rot.

Q. Would these differ at all if the floor was made of a softwood (Pine) or a hardwood (say, Oak)?

A. Yes. Hardwoods are more resistant to attack for longer than softwoods, but when wet enough are attacked by Death Watch Beetle: this beetle makes larger holes than Common Furniture beetle and does more damage, especially up the centre of the bearing ends.

- Look for the cause

Q. What is causing the creasing and lightening of the bearing ends?

A. Water getting in somewhere giving rise to rot

Q. How are you going to confirm that the cause is still present?

A. Use the ‘moisture meter’ but check it is calibrated for timber first. You may need long, insulated probes.

Q. Suggest the 'moisture meter' readings on which you might advise a Client as follows: a)no action required, b)at risk, needs treatment

A. a) below 16%  b) above 18% up to saturation at 28-32%

Q. Give as many examples as possible of where could the cause be coming from?

A. Penetrating damp from poor pointing, damaged bricks, cracked render, external balcony sealing defects, leaking downpipes and gutters Water leaks from internal pipework, central heating, mains water or sewerage, leaking shower trays or baths.

- Assess the damage

Q. How would you decide to what depth the timber is damaged?

A. Use your screw driver. Dig into the bearing as far as possible, particularly the lower edge.

Q. Approximately what proportion of the timber can be damaged and surface repaired, without needing to cut out the section?

A. Up to a maximum of one third of the cross sectional area, unless a Structural Engineer says otherwise. Some defects are more serious than others.

Q. Is damage more important in one part of the Joist than another, from a structural point of view?

A. Yes, the mid span of the Joist carries the largest bending load and because timber bends by compressing the upper half and stretching the lower half, so damage in the upper half is easier and safer to repair. Damage in the lower half usually needs rods to be embedded in order to resist the stretching or tension.

Also, the bearing of the Joist in the wall should be fixed to the wall head or wall plate to resist the outward movement of the wall - bowing. If the Joist Ends are badly rotted (particularly the lower half) the wall could, in theory, collapse. This ‘bowing’ load is also, in some floor designs, resisted by the addition of metal ties or mortar around the joist ends  – such mortar conducts moisture readily into the embedded ends, leading to rot. Always recommend a Structural Engineer if you see any signs of structural alteration or movement.

- Offer a repair

In one area there is slight surface damage: when dug out the missing wood measures 1 inch (25mm) x 1 inches (25mm) x 4 inches (100mm).

Q.  What volume in cc's or litres of repair product will you need and what type of product could you use?

A. 62.5cc or 0.0625 litres  of Mouldable Epoxy Mortar.

The bottom 1 foot (300mm) of 4 of the 8 inch (200mm) x 3 inch (75mm) Joist Ends are beyond repair.

Q. Which timber repair technique could you use to replace them?

A. Timber-Resin Splice – use a Type C for a Top Slot fixing, with top slots being cut on site, most commonly used where the ceilings are left in-situ. Or you could use a Type D where access is from below (from a basement or cellar). At the short cut off length of 300mm, if the joists actually sit inside the wall (rather than butt up to it, sitting on a ledge) a TRS Type C45 would be best – this incorporates a 45 degree face at the cut-off point.

Q. Which types of resin products are you likely to use?

A. For Top Slot repairs a Quick Setting Polyester Paste is used for the face joint. The Structural Resin is a Structural Epoxy Pouring Grout, poured directly into the slots.

Q. What techniques could be used to cut slots or holes into the remaining timber, for connection to a new piece?

A. Slots can be cut with an Auger or 3D Cutter in an electric drilling machine, with a chain saw or a slot cutting saw, using a chisel to clean out the roughed out slot.

Q. How much do you think the repair materials would cost?

A. For an 8 x 3 inch timber x 300mm 45 degree cut off made in softwood about £40.

Q. How long do you think it would take one man to cut out and replace one rafter foot?

A. Excluding travel, access, propping and making good about 0.5 hours.

Q. What types of treatment could you offer, to minimise the risk of future rot?

A. After repair, surface treat with Boron Gel to at least 300mm (12 inches) clear of all dampness (meter readings over 16%): if Dry Rot has been found also drill and inject Boron Paste.

Q. What other measures might you take, depending on the type of floor and ceiling materials, to reduce the risk of rot and insect attack?

A. Increase ventilation – basements and cellars (ground floor - air bricks), clear out all debris, support the bearing ends on plastic DPC material or plastic packing wedges, specify bearing end grain seal on the new timber part (TRS)

Course  help - David Moore - 01626 331351 - dcmoore@timber.org.uk

Site: ©1998 D C Moore
Page Design:- dcmoore@timber.org.uk